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	Material & Consumable Approval Matrix
	WMS-C-09



The definitive statement of which parent material and filler combinations IDM may weld. A combination not listed here is not weldable at IDM, whatever a drawing says, until it is added by the RWC.
	Parent material A
	Parent material B
	Process
	Filler / consumable
	WPS ref
	WPQR ref
	Approved

	Carbon steel
	Carbon steel
	MAG 135
	 
	WPS-IDM-CS-01
	WPQR/21033/TJ1
	Yes

	Carbon steel
	Carbon steel
	MAG 135
	 
	WPS-IDM-CS-02
	WPQR/21033/TJ2
	Yes

	Carbon steel
	Carbon steel
	TIG 141
	 
	WPS-IDM-CS03-BW
	WPQR/TUV/22477/TC3
	Yes

	Carbon steel
	Carbon steel
	TIG 141
	 
	WPS-IDM-CS04-FW
	WPQR/TUV/22477/NCH4
	Yes

	Stainless 316/316L
	Stainless 316/316L
	TIG 141
	 
	WPS-IDM-SS01-BW
	WPQR/TUV/22477/NCH5
	Yes

	Stainless
	Stainless
	TIG 141
	 
	WPS-IDM-SS02-FW
	WPQR/TUV/22477/NCH6
	Yes

	Mild steel
	Cast iron
	[TBC]
	Pure nickel
	NONE
	NONE
	NO

	 
	 
	 
	 
	 
	 
	 

	 
	 
	 
	 
	 
	 
	 

	 
	 
	 
	 
	 
	 
	 

	 
	 
	 
	 
	 
	 
	 

	 
	 
	 
	 
	 
	 
	 

	 
	 
	 
	 
	 
	 
	 



The mild steel to cast iron row is recorded as NOT APPROVED. It appears on the Alstom 24308 estimate headed "Trial #2", which implies a Trial #1. Establish what was welded on Trial #1 and where it went. Nothing further is welded in that combination until the RWC has qualified a procedure and qualified the welders, or formally excluded it.
Consumable classifications are left blank — enter them from the consumable certificates rather than from a WPS transcription.
	Role
	Name
	Signature
	Date

	Prepared by
	 
	 
	 

	RWC — approved
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